**Front Matter**

Title

Long Title: Interfacial-Redox-Induced Tuning of Superconductivity in YBa2Cu3O7-δ

Short Title: Interfacial Tuning of Superconductivity in YBCO

**Authors**

Peyton D. Murray,1ξ Dustin A. Gilbert,2ξ Alexander J. Grutter,2 Brian J. Kirby,2 David Hernandez-Maldonado,3 Maria Varela,3 Zachary E. Brubaker,1,4 Rajesh V. Chopdekar,5,6 Valentin Taufour,1 Rena J. Zieve,1 Jason R. Jeffries,7 Elke Arenholz,6 Yayoi Takamura,5 Julie A. Borchers,2 Kai Liu1,8\*

**Affiliations**

1Physics Department, University of California, Davis, CA 95616, USA.

2NIST Center for Neutron Research, National Institute of Standards and Technology, Gaithersburg, MD 20899, USA.

3Universidad Complutense de Madrid, Madrid 28040, Spain.

4Materials Science Division,Lawrence Livermore National Laboratory, Livermore, CA 94550, USA.

5Department of Materials Science and Engineering, University of California, Davis, CA 95616, USA.

6Advanced Light Source, Lawrence Berkeley National Laboratory, Berkeley, CA 94720, USA.

7Physics Division,Lawrence Livermore National Laboratory, Livermore, CA 94550, USA.

8Physics Department, Georgetown University, Washington, DC 20057, USA.

\* Corresponding author: [Kai.Liu@georgetown.edu](mailto:Kai.Liu@georgetown.edu)

ξ These authors contributed equally to this work.

**Abstract**

Novel approaches for modifying ion distributions in the solid-state offer unprecedented control over material properties, enabling the development of multifunctional materials. We report a scalable approach allowing for total control of the superconducting transition in films of optimally doped YBa2Cu3O7-δ (YBCO) via a chemically-driven ionic migration mechanism. In our approach, a Gd cap is deposited onto epitaxial YBCO films. The extremely high oxygen affinity of Gd initiates a solid-state redox reaction at the interface, removing oxygen from deep within the YBCO. Progressive reduction of the superconducting transition is observed, with complete suppression possible for a sufficiently thick Gd layer. These effects arise from the combined impact of redox-driven electron doping and the disruption of the YBCO microstructure due to oxygen migration and depletion. This work demonstrates an effective approach for tuning the superconducting properties of cuprates and extends the viability of ionic control over the superconductivity to the quasi-bulk regime.

**MAIN TEXT**

**Introduction**

Many of the properties of the high- copper oxide superconductors are strongly influenced by charge doping (*1*, *2*). The ability to control the doping level in these materials is therefore important not only for the development of experimental platforms that enable studies of correlated electron physics, but for multifunctional device applications as well. While traditionally (*3*–*6*) the doping level is fixed during synthesis via chemical substitution or post-growth annealing, recently several techniques have demonstrated approaches which allow for on-demand control. By leveraging electrolytic double layer techniques, gating experiments (*7*, *8*) on RBa2Cu3O7-δ (R=Y, Nd) thin films have achieved control over the Cu-site doping level, which determines the dominant electronic order, by introducing oxygen vacancies into the film under electric fields. In these materials, O2- ions can migrate under the influence of an externally applied electric field to eventually escape through the film surface, resulting in the formation of oxygen vacancies. To maintain charge neutrality electrons are returned to the Cu ions within the film, resulting in a reduction in Cu valence and reducing the hole concentration of the oxide. Signatures of the effects on the electronic order in these materials are profound, and point to the efficacy of oxygen migration and vacancy formation in manipulating the properties of the cuprate superconductors. Recently, we demonstrated a different, solid-state approach to manipulate ionic distributions in oxide thin films by using a reactive Gd capping layer and thus achieved ionic control of magnetism (*9*–*11*). Leveraging the reactivity of Gd, these capping layers can extract oxygen from an adjacent oxide film, with the level of oxygen depletion controlled by the thickness of the Gd and the ion mobility in the oxide, often at room-temperature. Superconducting YBa2Cu3O7-δ (YBCO) is a prototypical example of the high- cuprates, with crystal structure and electronic ordering sensitive to oxygen stoichiometry. Combined with its high ionic conductivity (*12*, *13*), these properties make it an ideal candidate material to explore with this method.

In this study Gd capping layers of varying thicknesses are deposited on 100 nm thick YBa2Cu3O7-δ films, dramatically altering the oxygen distribution throughout the underlying film without any annealing. As the Gd layer thickness () is increased the YBCO layer becomes progressively more oxygen deficient, demonstrating how appropriate tuning of can precisely control the remaining oxygen content of the underlayer. The extraction of oxygen from the YBCO alters the superconductivity by reducing and broadening the superconducting transition, with superconductivity being completely extinguished for the sample with thickest capping layer. Differences between the superconducting transitions observed in resistivity and magnetometry suggest the formation of a percolative network of oxygen deficient regions alongside the nominally stoichiometric YBCO. X-ray diffraction (XRD) patterns show an expansion in the *c*-axis lattice parameter consistent with oxygen depletion, while x-ray absorption spectra (XAS) indicate a reduction of Cu valence state consistent with the removal of oxygen from deep within the YBCO film, and particularly from within the CuO chains. Since superconductivity in YBCO relies on charge transfer from the CuO chains to the CuO2 planes, the disappearance of superconductivity may be in part due to the reduction in hole doping level. At the same time, STEM images indicate the presence of stacking defects associated with other structural phases with lower . Whether due to redox-driven electron doping or structural changes, both effects are induced by Gd-driven oxygen migration.

**Results**

Commercially available films of pulsed-laser-deposited YBa2Cu3O7-δ (100 nm) grown on (001) SrTiO3 (STO) substrates were purchased for this experiment (*14*). The high-symmetry STO substrate (cubic, lattice parameter of 3.905 Å) is known to yield YBCO films with 90° twinned domains (*15*), with up-to 2% tensile strain exerted at the interface due to lattice mismatch (*16*, *17*) (bulk lattice parameters of YBCO are *a* = 3.827 Å, *b* = 3.893 Å, and *c* = 11.699 Å (*18*)). While the strain is known to suppress , the films are expected to relax away from the substrate/film interface (*19*, *20*) and show near bulk-like superconducting behavior (*17*). The films were then sputter coated with Gd layers of varying thickness ( 3 nm, 7 nm, 20 nm) and an Au (5 nm) protective cap, with one witness sample of YBCO/STO kept in the as-grown state for comparison.

X-ray diffraction (XRD) scan of the as-grown film (Fig. 1A) shows only the family of peaks, corresponding to a lattice parameter of *c* =11.678 Å, similar to the bulk value of 11.699 Å (*18*). The slightly smaller *c*-axis lattice parameter may be due to the tensile strain from the substrate (*21*). As is increased, a monotonic shift towards lower is observed in the YBCO diffraction peaks, indicating expansion in the *c*-axis, similar to those previously reported in other perovskite systems (*22*) as a signature of oxygen depletion. Between the and nm samples, a significant shift and broadening of the peaks is observed, indicating further *c*-axis expansion as well as disruption of the crystalline structure. In addition to the out-of-plane direction, the in-plane structure of the films was probed using reciprocal space maps (RSMs) taken near the STO substrate reflection (Figs. 1B-E, G-J). Coordinates of the RSMs identify the *h* (*x*-axis) and *l* (*y*-axis) Miller indices relative to the STO substrate. When grown on cubic STO substrate, nominally orthorhombic YBCO is expected to form a twinned crystal structure, resulting in a splitting of the in-plane Bragg reflections (*16*). For each sample, the RSM shows a bright substrate peak (Figs. 1B-E), with the multiple peaks observed in the nm and 7 nm samples likely due to impurities. Each of the nm, 3nm, and 7 nm samples also shows a lower-intensity, broadened YBCO peak near ; for this peak is absent. Owing to the nearly identical in-plane lattice parameters, two closely spaced Bragg reflections are expected from the and YBCO crystal planes; however, only a single peak is observed in the as-grown YBCO (Fig. 1G). The center of this peak is displaced towards more negative values of than the STO peak, meaning these films are relaxed in-plane before Gd capping layers are deposited. As is increased, the YBCO film peak broadens along the (00*l*) direction and shifts to lower , consistent with an expansion in the *c*-axis lattice parameter discussed above.

The effects of Gd deposition on the YBCO superconducting properties were investigated by magnetometry and Van der Paw resistivity. Zero-field cooled (ZFC) magnetometry measurements were carried out by first cooling each sample in zero field to 5 K before applying a 10 Oe magnetic field. The magnetic moment was then measured as the sample warmed from 5 K back to 100 K. The magnetometry of the as-grown YBCO film (Fig. 2) shows a sharp superconducting transition at K, which is typical of YBCO films grown on STO substrates (*17*). Below , the moment saturates as the Meissner effect causes all externally applied magnetic fields to be expelled from the sample. Accompanying the magnetic transition is a precipitous drop in resistivity to zero, further confirming the superconducting transition. With increasing Gd capping layer thickness the magnetic transition shows a smooth reduction in the magnetic transition temperature , to 62 K for and 36 K for , with complete suppression of the Meissner effect for nm. In contrast to the magnetometry, resistivity measurements initially show only a small shift toward lower for nm. However, for nm and nm the resistive superconducting transition is completely suppressed, with no apparent transition down to the lowest measured temperature (5 K).

While resistivity probes a contiguous superconducting path, magnetometry is sensitive to bulk Meissner effect. The different temperature dependence observed in magnetometry and resistivity therefore reflects different properties of the YBCO, with magnetometry equally sensitive to regions with any , and resistivity sensitive only to the regions of the film with highest – so long as a superconducting path is maintained. The observed transitions can be explained by the presence of an oxygen-deficient (OD) phase with lower , stabilized alongside the optimally doped (OP) YBCO phase. For the nm sample most of the film possesses the initial structure and nominal stoichiometry of YBa2Cu3O7-δ, meaning a contiguous path through the OP phase still exists, and the resistive transition is observed close to the of the as-grown film. By comparison, the nm sample shows a transition in the magnetometry, but not in the resistivity. Therefore, the nm sample possesses some OD phase fraction which is still superconducting at a lower , as seen in magnetometry, but is beyond the percolation limit for the resistive OD phase, as evidenced by the absence of a transition in the resistance. Finally, for the thickest nm sample the absence of a transition in either the resistance or magnetic data suggests few, if any, regions undergo superconducting transition in the sample. The distinctly different superconducting properties of the OD phase may be the result of structural changes or electron doping, both of which are consequences of the oxygen leaching.

The Gd capping layer is expected to extract oxygen from the YBCO, resulting in the structural changes that were observed in XRD patterns. Cross-sectional high-angle annular dark field scanning transmission electron microscopy (HAADF-STEM) images of the as-grown film at the STO/YBCO interface show flat, epitaxial YBCO growth consistent with XRD patterns. The layered structure of YBa2Cu3O7-δ is well resolved (Fig. 3A-C), with the crystal structures of the substrate (Fig. 3A inset) and the YBCO film (Fig. 3B, C insets) labeled in color. Multi-CuO layer stacking faults, which disrupt the crystallinity, are distributed throughout the imaged regions (Fig. 3A-C). Examples of similar double-CuO stacking faults have been previously reported in laser deposited films of YBCO (*23*–*25*), where they have been attributed to the limited atomic diffusion range under typical laser deposition conditions. Double- or multi-CuO stacking faults form different microstructural phases than optimally doped YBa2Cu3O7-δ (Y-123, with numbers denoting cation stoichiometry), e.g. Y-124 and Y-247. These defects directly alter the CuO chains, which act as charge reservoirs for superconductivity in the YBCO system. Accordingly, these types of defects affect the superconducting transition, and result in lowered critical temperatures as compared to Y-123 (*26*–*29*). These stacking faults point to the aggressive nature of the oxygen leaching effect, as the YBCO layers become increasingly disrupted when oxygen is removed from deep within the film, and suggest that changes to the microstructure likely play a key role in the suppression of superconductivity.

The extraction of oxygen was further probed by polarized neutron reflectometry (PNR), which provides a depth-resolved mapping of the nuclear scattering centers within the film. The converged depth profiles (Fig. 4) confirm the nuclear scattering length density (SLD, ) of the as-grown film is similar to the calculated value for YBa2Cu3O7 of . With increasing the YBCO layer increases in thickness, in qualitative agreement with the unit cell expansion observed in XRD. Commensurate with the progressive increase in thickness, the nuclear SLD decreases, particularly near the YBCO/Gd interface, consistent with the removal of oxygen from the YBCO. In addition to the real part of the nuclear profile, the Gd layer is explicitly identifiable by the imaginary component of its SLD, which corresponds with neutron absorption. Since Gd is the only significant neutron absorber present in this system, the imaginary component of the nuclear SLD allows us to rule out the possibility of YBCO/Gd interdiffusion.

While the PNR results are consistent with the extraction of oxygen from the YBCO, fluorescence yield (FY) XAS measurements performed at the Cu *L*2,3-edges directly confirm a change in the Cu valence resultant from the oxygen extraction. The XA results (Fig. 5) show a shift in the absorption resonance to lower energies with increasing . Similar spectral shifts reported in other oxygen-deficient perovskite systems (*30*, *31*) have been attributed to a decrease in the average Cu valence, the result of electrons returning to the Cu ions as oxygen is leached from the film. The shoulder at eV in the as-grown YBCO spectra, a feature characteristic of lower-valence ligand states present in CuO chains (*8*, *32*–*34*), is suppressed for greater , confirming the loss of oxygen within the chains. A second resonance associated with the Cu1+ valence state emerges at eV for 7 nm and 20 nm. This new absorption peak, appearing in conjunction with the emergent low angle feature observed in XRD, again points to the formation of a stable OD phase. The bulk sensitivity of FY measurements (70% X-ray transmission through 100 nm of YBCO at Cu-*L*2 resonance) infers that the observed oxygen depletion comes from ionic migration from deep within the film despite the interfacial origin of the leaching effect. The high ionic conductivity required for such long-range oxygen migration is in agreement with previous reports (*12*, *13*). The known sensitivity of the YBCO superconductivity to the oxygen stoichiometry suggests that this approach may therefore be used as a mechanism to design the superconducting transition.

**Discussion**

In summary, two different mechanisms may contribute to the suppression of superconductivity. The first mechanism is electron doping; as observed in XAS, the more oxygen stripped away by the adjacent Gd capping layer, the more the Cu valence state decreases. This electron doping effectively shifts the YBCO film from the optimally doped state, where is maximized, back towards the electron-doped region of the global phase diagram, with a corresponding decrease in . Magnetometry shows that for intermediate capping layer thicknesses, the superconducting transition broadens across a range of temperatures, indicating regions with a distribution of coexist within the same film. The second mechanism involves the disruption to the film microstructure. The crystal structure of optimally doped YBCO contains both CuO2 planes – where superconductivity resides – and CuO chains, which act as the doping centers for the planes. As oxygen is removed from the film, the chains become progressively more oxygen deficient, with resulting defects observed via STEM. The presence of double- and multi-CuO stacking faults directly modifies these doping centers, locally forming separate structural phases with lower values of .

In summary, Gd capping layers deposited at room temperature on optimally doped YBCO thin films have been shown to remove oxygen from the underlying film via an interfacial redox reaction, with the extent dependent on capping layer thickness. This redox-induced oxygen migration results in a percolative phase transformation from the optimally doped state to an oxygen deficient state which does not support superconductivity. As measured in magnetometry and resistivity, the superconducting transition temperature is significantly reduced with increasing Gd thickness, and for sufficiently thick capping layer, the transition is extinguished completely. Spectroscopic measurements reveal the loss of oxygen with the CuO chains as well as a decrease in the average Cu valence, indicating that oxygen leaching effectively acts to electron dope the YBCO, decreasing . Meanwhile, STEM images reveal the presence of defects associated with separate, oxygen-deficient structural phases, suggesting that both changes to the microstructure as well as a reduction in hole doping level may play roles in the suppression of superconductivity. Remarkably, the changes to the superconducting properties throughout the entire 100 nm thick YBCO films are induced by the migration of oxygen towards the YBCO/Gd interface, extending the viability of this approach for controlling the hole-doping level to the quasi-bulk regime.

**Materials and Methods**

**Film growth and characterization**

Commercially available 100 nm thick YBCO films grown on STO substrates were purchased from MTI Corporation for this experiment. The films, which were delivered and kept in a vacuum-sealed box prior to Gd deposition, were exposed to atmosphere for < 1 h before being transferred to a high vacuum environment, where they were sputter coated with Gd (3 nm, 7 nm, 20 nm) and a Au (5 nm) protective capping layer using Ar gas at Pa working pressure in a chamber with a base pressure of Pa. XRD characterization, including both symmetric scans and reciprocal space maps, was performed on a X-ray diffractometer equipped with parallel beam optics and Cu monochromator. Polarized neutron reflectometry was measured at the NIST Center for Neutron Research on the PBR and MAGIK beamlines. The experiment used 5 Å neutrons, and were carried out at a temperature of 6 K. Fitting of the PNR data was performed using the Refl1d software package, following a Markov-chain Monte Carlo fitting algorithm (*35*). The calculated SLD was determined by the calculating the sum of the volume-scaled atomic scattering lengths. XA measurements were performed at the Advanced Light Source on beamline 4.0.2 at room temperature in a grazing incidence (30°) geometry. Both fluorescence and electron yield (EY) modes were measured, but due to the capping layers no appreciable signal was measured in the EY mode. Magnetometry measurements were performed by first cooling the samples to 5 K in zero field; a field of 1 mT was then applied, and the magnetic moment was recorded as the sample warmed back to 100 K. To reduce stray magnetic fields, the magnet was purged before each measurement. The transition temperatures quoted from the magnetometry were acquired by taking the midpoint of the curves. Resistivity was measured using a four-contact Van der Pauw geometry. The current used was 100 µA at frequency of 173 Hz. The magnetic field at the sample was set to zero before the measurement by setting the temperature to the midpoint of the superconducting transition before adjusting the applied field to minimize the resistivity.

References

1. R. J. Cava *et al.*, Structural anomalies at the disappearance of superconductivity in Ba2YCu3O7−δ: Evidence for charge transfer from chains to planes. *Phys. C Supercond.* **156**, 523–527 (1988).

2. S. Blanco-Canosa *et al.*, Resonant X-ray Scattering Study of Charge Density Wave Correlations in YBa2Cu3O6+x. *Phys. Rev. B*. **90**, 054513 (2014).

3. M. R. Presland, J. L. Tallon, R. G. Buckley, R. S. Liu, N. E. Flower, General trends in oxygen stoichiometry effects on Tc in Bi and Tl superconductors. *Phys. C Supercond. its Appl.* **176**, 95–105 (1991).

4. P. A. Lee, N. Nagaosa, X. G. Wen, Doping a Mott insulator: Physics of high-temperature superconductivity. *Rev. Mod. Phys.* **78** (2006).

5. W. A. Groen, D. M. de Leeuw, G. P. J. Geelen, Hole concentration and Tc in Bi2Sr2CuO6+δ. *Phys. C Supercond. its Appl.* **165**, 305–307 (1990).

6. R. G. Humphreys *et al.*, Physical vapour deposition techniques for the growth of YBa2Cu3O7 thin films. *Supercond. Sci. Technol.* **3**, 38–52 (1990).

7. A. M. Perez-Muñoz *et al.*, In operando evidence of deoxygenation in ionic liquid gating of YBa2Cu3O7-X. *Proc. Natl. Acad. Sci.* **114**, 215–220 (2017).

8. L. Zhang *et al.*, The Mechanism of Electrolyte Gating on High-Tc Cuprates: The Role of Oxygen Migration and Electrostatics. *ACS Nano*. **11**, 9950–9956 (2017).

9. D. A. Gilbert *et al.*, Controllable positive exchange bias via redox-driven oxygen migration. *Nat. Commun.* **7**, 11050 (2016).

10. A. J. Grutter *et al.*, Reversible control of magnetism in La0.67Sr0.33MnO3through chemically-induced oxygen migration. *Appl. Phys. Lett.* **108** (2016), doi:10.1063/1.4942645.

11. D. A. Gilbert *et al.*, Structural and magnetic depth profiles of magneto-ionic heterostructures beyond the interface limit. *Nat. Commun.* **7**, 12264 (2016).

12. G. J. Shen, C. C. Lam, J. C. L. Chow, S. T. Tang, Twin formation due to irradiation of energetic electron beam in high-temperature superconductors of In- and Sb-doped YBCO. *Phys. C Supercond. its Appl.* **214**, 426–434 (1993).

13. J. H. Muller, W. Mertin, R. Gruehn, Oxygen mobility in YBa2Cu3O7-x: A TEM and HRTEM investigation. *Supercond. Sci. Technol.* **3**, 273–281 (1990).

14. M. Lorenz *et al.*, High-quality Y-Ba-Cu-O thin films by PLD-ready for market applications. *IEEE Trans. Appiled Supercond.* **11**, 3209–3212 (2001).

15. J. M. Phillips, Substrate selection for high-temperature superconducting thin films. *J. Appl. Phys.* **79**, 1829–1848 (1996).

16. J. D. Budai, R. Feenstra, L. A. Boatner, X-ray study of in-plane epitaxy of YBa2Cu3Ox thin films. *Phys. Rev. B*. **39**, 12355–12358 (1989).

17. H. Y. Zhai, W. K. Chu, Effect of interfacial strain on critical temperature of YBa2Cu3O7-δ thin films. *Appl. Phys. Lett.* **76**, 3469–3471 (2000).

18. G. Calestani, C. Rizzoli, Crystal structure of the YBa2Cu3O7 superconductor by single-crystal X-ray diffraction. *Nature*. **328**, 606–607 (1987).

19. W. J. Lin, P. D. Hatton, F. Baudenbacher, J. Santiso, Observation of small interfacial strains in YBa2Cu3Ox sub-micron-thick films grown on SrTiO3 substrates. *Appl. Phys. Lett.* **72**, 2966–2968 (1998).

20. F. M. Granozio, F. Ricci, U. Scotti di Uccio, J. C. Villegier, Orthorhombic-tetragonal transition in twin-free (110) YBa2Cu3O7 films. *Phys. Rev. B*. **57**, 6–9 (1998).

21. C. Xie, J. I. Budnick, B. O. Wells, J. C. Woicik, Separation of the strain and finite size effect on the ferromagnetic properties of La0.5Sr0.5CoO3 thin films. *Appl. Phys. Lett.* **91**, 172509 (2007).

22. S. Miyoshi *et al.*, Lattice expansion upon reduction of perovskite-type LaMnO3 with oxygen-deficit nonstoichiometry. *Solid State Ionics*. **161**, 209–217 (2003).

23. R. Ramesh *et al.*, Direct Observation of Structural Defects in Laser-Deposited Superconducting Y-Ba-Cu-O Thin-Films. *Science*. **247**, 57–59 (1990).

24. L. F. Fu *et al.*, Interface and defect structures in YBa2Cu3O7-δ and Nb:SrTiO3 heterojunction. *J. Phys. D. Appl. Phys.* **40**, 187–191 (2007).

25. R. Ramesh *et al.*, Defect Structure of Laser Deposited Y-Ba-Cu-O Thin Films on Single Crystal MgO Substrate. *J. Mater. Res.* **5** (1990), doi:10.1557/JMR.1990.0704.

26. R. J. Cava *et al.*, Bulk Superconductivity at 91 K in Single-Phase Oxygen-Deficient Perovskite Ba2YCu3O9-δ. *Phys. Rev. Lett.* **58**, 1676–1679 (1987).

27. P. Bordet, C. Chaillout, J. Chenavas, J. Hodeau, Structure determination of the new high-temperature superconductor Y2Ba4Cu7O14+x. *Nature*. **334**, 596–596 (1988).

28. D. E. Morris *et al.*, Synthesis and properties of the 2:4:7 superconductors R2Ba4Cu7O15-x (R=Y, Eu, Gd, Dy, Ho, Er). *Phys. Rev. B*. **40**, 11406–11409 (1989).

29. D. E. Morris *et al.*, Eight new high-temperature superconductors with the 1:2:4 structure. *Phys. Rev. B*. **39**, 7347–7350 (1989).

30. B. Li *et al.*, Tuning interfacial exchange interactions via electronic reconstruction in transition-metal oxide heterostructures. *Appl. Phys. Lett.* **109**, 152401 (2016).

31. N. Lu *et al.*, Electric-field control of tri-state phase transformation with a selective dual-ion switch. *Nature*. **546**, 124–128 (2017).

32. C. T. Chen *et al.*, Out-of-plane orbital characters of intrinsic and doped holes in La2-xSrxCuO4. *Phys. Rev. Lett.* **68**, 2543–2546 (1992).

33. N. Nücker *et al.*, Site-specific and doping-dependent electronic structure of YBa2Cu3Ox probed by O 1s and Cu 2p x-ray-absorption spectroscopy. *Phys. Rev. B*. **51**, 8529–8542 (1995).

34. A. Bianconi *et al.*, Localization of Cu 3d levels in the high Tc superconductor YBa2Cu3O~7 by Cu 2p X-ray photoelectron spectroscopy. *Solid State Commun.* **63**, 1135–1139 (1987).

35. B. J. Kirby *et al.*, Phase-sensitive specular neutron reflectometry for imaging the nanometer scale composition depth profile of thin-film materials. *Curr. Opin. Colloid Interface Sci.* **17**, 44–53 (2012).

**Acknowledgments:** This work has been supported by the NSF (DMR-1610060 and ECCS-1611424). Work at LLNL has been supported by the DOE (DE-AC52-07NA27344) and NSF (DMR-1609855).

**Author contributions:** P.D.M., D.A.G. and K.L. coordinated the project. P.D.M. synthesized the samples, carried out structural analysis, and prepared the first draft of the manuscript. D.A.G., A.J.G., B.J.K, and J.B. performed PNR studies. D.A.G. and A.J.G. and E. A. carried out XAS measurements. D. H-M. and M.V. carried out electron microscopy studies. V. T. measured magnetometry. Z.E.B., J.R.J., and R. Z. carried out transport measurements. R.V.C. and Y.T. assisted with sample synthesis and RSM studies. All authors contributed to data analysis and manuscript revision. **Competing interests:** The authors declare no competing interests. **Data and materials availability:** Experimental data is available upon request.

**Figures**


**Fig 1**. **X-ray diffraction.** (**A**) XRD scan near the (002) YBCO peak measured with Cu radiation. Reciprocal space maps showing (**B-E**) the () STO substrate peak, (**G-J**) YBCO peak, and (**F, K**) projections of each map along the -direction.

**Figure 2**. **Magnetization and resistivity.** Normalized magnetization (**A**) and resistivity (**B**) from 5 K to 100 K. The Gd (20 nm) sample has been omitted from (**B**), as no magnetic moment was detected at any temperature measured (to within experimental noise).


**Figure 3**. **STEM images.** Cross-sectional HAADF-STEM images of the as-grown STO/YBCO interface (**A**) with a magnified view of the substrate/film interface shown in the inset. The crystal structure is depicted with Cu, Ba, Y, Sr, and Ti atoms highlighted in yellow, red, blue, violet, and orange, respectively. The YBCO/Gd interface of the Gd (3 nm) (**B**) sample with a magnified view of a CuO stacking fault shown in the inset. Center of the YBCO layer in the Gd (20 nm) film (**C**), with a magnified view of the crystal. Dashed red lines highlight double- or multi-CuO stacking faults.

**Figure 4**. **Polarized Neutron Reflectometry.** Real and imaginary components of the nuclear SLDs as a function of depth through the (**A**) as grown, (**B**) Gd (3 nm), (**C**) Gd (7 nm), and (**D**) Gd (20 nm) samples as measured by PNR. Grey region () corresponds to the substrate, with the approximate location of the YBCO, Gd, and Au layers given by the shaded regions for (). The nominal SLD of optimally doped YBa2Cu3O7-δ is shown by the grey line in each panel.


**Figure 5**. **X-ray Absorption Spectra.** Close-up view of the normalized absorption spectra as a function of incident X-ray photon energy near the Cu -edge, as measured in fluorescence yield mode. The full spectral range measured including the Cu -edge is shown in the inset, with the shaded region corresponding to the close-up view.




**Fig. 1**




**Fig. 2**



**Fig. 3**



**Fig. 4**



**Fig. 5**