## Slide 1
Peak from Cu1+ state

## Slide 2
YBa2Cu3O7
(3Cu7/3+=2Cu2+ + Cu3+)
YBa2Cu3O6.5
(3Cu2+)
YBa2Cu3O6
(3Cu5/3+=2Cu2++Cu1+)

## Slide 3
Emergent New Phase?

## Slide 4
YBCO As Grown
YBCO/Gd(3 nm)

## Slide 5
YBCO/Gd(7 nm)
YBCO/Gd(20 nm)

## Slide 7
The story so far:
XAS shows that with increased Gd we develop an emergent Cu1+ peak
There are stable, oxygen deficient phases of YBCO
YBa2Cu3O7 has is a mixed valence (+2 and +3); YBa2Cu3O6.5 as Cu2+ valence; YBa2Cu3O6 has a mixed (2+ and 1+)
Thus XAS implies we took out at-least 1 oxygen ion per unit cell (which is a lot)
XRD shows a shift in the peak initially, indicating simple lattice expansion. For YBCO/Gd(7nm and 20 nm) a new peak is emergent, indicating the likely formation of a new phase.